## Slide 1: X-56A
Wing Box Construction
  Upper and Lower Panels
    S-2 Fiberglass – typically 2-3 ply face sheets
    Rohcell foam core – typically 0.25” (some 0.375”)
    Leading edge is separate part, solid laminate
  Leading and Trailing Spars
    Flat web with caps
    Solid Laminate carbon fiber – [45,0,45]s
  Ribs
    Flat web with caps
    Carbon Fiber – typically 2-3 ply face sheets
    Mix of solid laminate and Rohcel foam core – typically 0.375”
Wing Molds:
Upper Skin
Lower Skin
Leading Edge
Front Spar
Aft Spar
Ribs (?)
Control Surfaces

## Slide 2: mAEWing2 Desired
Desire is to mimic a wing box structure with Ribs
  Reduce number of molds required for fabrication
    Use flat stock or a common custom ply layup for all parts
    1/8” Core in flat stock, could do custom in skins
  Simplify and Standardize where possible
Very limited design space
  Some flexibility in placement and sizing of spars
  Rib placement and sizing
  Limited material selection
Froude Scaling as a Guide – 12ft (correcting to 0.125” core)
  Carbon (IM7) in X-56A
    E = 76 GPa, G = 3.8GPa - scales to - E = 21 GPa, G = 1.2 GPa
    E-glass fiber is a decent match: E = 23 GPa, G = 3.5 GPa
  Fiberglass (S-2 Glass) in X-56A
    E = 28 GPa, G = 3.5 GPa - scales to - E = 7.6 GPa, G = 1.1 Gpa
    Unobtainium?? (Vacuum formed thermoplastic ?)
Wing Molds:
Upper Skin (ambidex)
Lower Skin (ambidex)
Leading Edge (?)

## Slide 3: mAEWing2 Alternative 1
Alternate Concept
  Use flat stock or a common custom ply layup for all parts
  No Ribs
  No Molds – Layup over foam core with spars
  Requires the skins to carry the loads
    Still may not be feasible without unobtainium
      Unobtainium is limited to fabric carried thermo-sets due to temperature and pressure constraints
Very limited design space
  Some flexibility in placement and sizing of spars
  Material selection

## Slide 4: mAEWing2 Alternative 2
Alternate Concept
  Same as BFF and MiniMUTT
  No Ribs
  No Molds – Layup over foam core with spar
  Requires the skins to carry the loads
Limited design space
  Spar placement, sizing, and materials vary the response significantly